	Texaco

Technology

Ghent
	


	Termék

Információ

	11/05/2000
	
	

	BIOSTAR HYDRAULIC


Leírás

BIOSTAR HYDRAULIC biolebontható, cinkmentes (hamumentes) repceolaj alapú HTG hidraulikaolaj. Speciálisan azon felhasználók számára fejlesztették ahol fennáll a környezetszennyezés lehetősége a felhasználás során.
Előnyök

BIOSTAR HYDRAULIC kielégíti a CEC-L-33-A-93 szabvány szerinti magasfokú biolebonthatóságot, “VÍZ VESZÉLYESSÉGI FOKOZAT” 0 osztályú ( tehát a legjobb).

BIOSTAR HYDRAULIC hidraulika olajnak nagyon jó az oxidáció stabilitása és a oxidáció gátló képessége. Kíváló kopásgátló tulajdonsággal rendelkezik.

BIOSTAR HYDRAULIC hidraulika olajnak jó a viszkozitás-hőmérséklet karakterisztikája, azaz széles hőmérsékleti tartományban alkalmazható. Alkalmazható :

      -15C és +80C között.

BIOSTAR HYDRAULIC hidraulika olaj használata mindazon helyeken ajánlott ahol, a környezet szennyezés lehetősége fenn áll.

BIOSTAR HYDRAULIC hidraulika olaj összeférhető a hidraulikus rendszerekben használatos tömítésekkel, valamint keverhető a konvencionális ásványolaj alapú hidraulikus folyadékekkal.

Megjegyzés

A megadott termékjellemzők tipikus adatok. A gyártó fenntartja a jogot a jellemzők megváltoztatására.

	
	


	PRODUCT

INFORMATION

	
	TYPICAL DATA


	

	BIOSTAR HYDRAULIC


	Viscosity Grade
	
	32
	46

	Code number
	
	32087
	32088

	ETL - number
	Test methods
	6648
	6740

	Appearance
	Visual
	Clear Liquid
	Clear Liquid

	Visc. Kinematic @0Deg C
	ISO 3104
	207
	341

	Visc. Kinematic @20Deg C
	ISO 3104
	890
	1596

	Visc. Kinematic @40Deg C
	ISO 3104
	32.63
	46.2

	Visc. Kinematic @100Deg C
	ISO 3104
	7.53
	10.1

	Visc. Index
	ISO 2909
	210
	210

	Color
	ISO 2049 
	1
	1.5

	Flash Point, Deg C
	ISO 2592
	210
	225

	Pour point, Deg C
	ISO 3016
	-30
	-30

	Density, 15 Deg C, Kg/l
	ASTM D0941 
	0.918
	0.925

	Air Release @50 Deg C, min
	ISO DIS 9120
	5
	7

	Foam Seq. I, IAB ml
	ISO 6247
	0
	0

	Foam Seq. I, AFT 10 ST ml
	ISO 6247
	0
	0

	Foam Seq. II, IAB ml
	ISO 6247
	0
	0

	Foam Seq. II, AFT 10 ST ml
	ISO 6247
	0
	0

	Foam Seq. III, IAB ml
	ISO 6247
	0
	0

	Foam Seq. III, AFT 10 ST ml
	ISO 6247
	0
	0

	Cu Corrosion, 3h, 100 Deg C
	ASTM D0130
	1B
	1B

	Demulsibility, 40-40 , min
	ASTM D1401
	40
	40

	Rust - distilled water
	ASTM D0665A
	Pass
	Pass

	Rust - seawater
	ASTM D0665B
	Pass
	Pass

	FZG Damaged Load, a/8.3/90
	DIN 51354
	12
	12

	Total Acid Number, mgKOH/g
	DEA Testmethod
	0.5
	0.5

	Phosphorus, %w
	XRAY
	0.0090
	0.0090

	Zinc, %w
	XRAY
	0
	0

	Calcium, %w
	XRAY
	0
	0

	Sulphur, %w
	XRAY
	0.0150
	0.0150

	Elastomer Comp., 168h,100C
	
	.
	.

	_NBR-1 Hardness
	DIN 53505
	-4
	-5

	_NBR-1 Volume
	DIN 53521
	8
	8


	
	


	PRODUCT

INFORMATION

	
	TYPICAL DATA


	

	BIOSTAR HYDRAULIC


	Viscosity Grade
	
	32
	46

	Code number
	
	32087
	32088

	ETL - number
	Test methods
	6648
	6740

	WHC
	
	0
	0

	Vickers Vane Pump
	ASTM D2882
	Pass
	Pass

	Baader Oxide Test 72h 95C
	DIN 51554
	.
	.

	_VIS 40C, Increase, %
	
	10
	12

	_TAN Increase mgKOH/g
	ASTM D2664
	0.6
	0.5

	_VISC Kinematic 100Deg C mm2/s
	
	7.22
	9.59

	_Viscosity Loss %
	
	4.7
	5

	SON SHE 40C VIS CH
	ASTM D2603
	0.08
	0.46

	Filterability 75 ML 0% s
	DENISON    (2)
	180
	190

	Filterability 75 ML 2% s
	DENISON    (2)
	210
	221


HANDLING PRACTICES
For information on the safe handling and use of this product, refer to the Material Safety Data Sheet (available on the Texaco PSI Intranet Site).

	TEXACO TECHNOLOGY GHENT

	
	BIOSTAR HYDRAULIC
	( page 1 of 3)



_978506331.doc
�



�
















_978520863.doc
�



�
















